## Slide 1
Scanning Probe Microscopy across dimensions
I.C. Gebeshuber1,2, R.A.P. Smith2, HP. Winter2, F. Aumayr2
1Austrian Center of Competence for Tribology AC2T, Wiener Neustadt, Austria &
2Institut f. Angewandte Physik, Vienna University of Technology, Austria
Notes: Hallo!

## Slide 2
100m
10-1m
10-2m
10-3m
10-4m
10-5m
10-6m
10-7m
10-8m
10-9m
10-10m
10-11m
woman
small animal
lady bug
flea
amoeba
red blood cell
cholera bacterium
tobacco mosaic virus
large organic molecule
large molecule
atom
atom orbitals
light microscopy
scanning probe microscopy
transmission and scanning
electron microscopy
Gebeshuber I.C. et al. (2006) "Scanning Probe Microscopy: From living cells to the subatomic range", In: Applied Scanning Probe Methods III, Springer, 27-53.

## Slide 3
SPM methods
Cells:
  Diatoms
  Short excursion to biogenic adhesives
  Biotribology
Single molecules
  Chaperonins: Probing protein-protein
  interactions in real time
Atoms
  Nanostructuring atomically flat surfaces with ions
  Ion bombardment of atomically flat crystals
Subatomic features
  Atom orbitals
  Electron spins

## Slide 4
Some SPM methods

## Slide 5: Generalized scheme of an SPM
A scanning probe microscope (SPM) raster scans a sharp probe over a surface.
The mechanical, electrical, magnetic, optical and chemical interaction between the sharp probe and the surface provides a 3D representation of surface parameters at or near the atomic scale. The samples can be in air, vacuum, or immersed in some liquid.

## Slide 6: Some types of SPMs
Scanning tunneling microscopy (STM, 1982)
atomic force microscopy (AFM, 1984)
scanning near field optical microscope (SNOM, 1986)
magnetic force microscope (MFM)
magnetic resonance force microscope (MRFM)
scanning thermal microscope
scanning potentiometry microscope
ballistic electron emission microscope (BEEM)
scanning capacitance microcope
scanning ion conductance microscope (SICM)

## Slide 7: Scanning Probe Microscopes: Scanning Tunneling Microscopy
The STM measures a weak electrical current flowing between tip and sample (tunneling current).

## Slide 8: Scanning Probe Microscopes: Atomic Force Microscopy
The AFM measures the interaction force between the tip and surface.
The tip may be dragged across the surface, or may vibrate as it moves.
© P. Hansma, UCSB

## Slide 9: AFM operational modes
Contact mode
Non-contact mode
Intermittent mode
Phase imaging

## Slide 10: Scanning Probe Microscopes: Scanning Near Field Optical Microscopy
In SNOM, the excitation laser light is focused through an aperture with a diameter smaller than the excitation wavelength, resulting in an evanescent field (or near-field) on the far side of the aperture.

## Slide 11: Scanning Probe Microscopes: Scanning Near Field Optical Microscopy
When the sample is scanned at a small distance below the aperture, the optical resolution of transmitted or reflected light is limited only by the diameter of the aperture.
In particular, lateral resolution of 20 nm and vertical resolution of 2–5 nm have been demonstrated.

## Slide 12: Scanning Probe Microscopes: Scanning Near Field Optical Microscopy
The NSOM scans a very small light source very close to the sample.
Detection of this light energy forms the image.
NSOM can provide resolution below that of the conventional light microscope.

## Slide 13: Scanning Probe Microscopes: Scanning Ion Conductance Microscopy
The SICM measures the ion current between two electrodes, one in a sharp glass needle, one in the bath solution.
Resolution: half the diameter of the pipette. Great for biological samples.
© P. Hansma, UCSB

## Slide 14: Human Chromosomes
© Terry McMaster, Bristol University
AFM, 20.20 mm2

## Slide 15
Cells

## Slide 16: Cells: Diatoms
Single cellular organisms
Size: some micrometers
10 000s different species
Reproduce via cell division
Under ideal conditions, within ten days the offspring of one single cell number one billion cells (assembly line production of nanostructures)
Surfaces made from amorphous glass
© W. Oschmann

## Slide 18
Top: Tricaeratium favus, bottom left: Roperia tessellata,
bottom right: Achnathes brevipes © Gebeshuber et al., J. Mat. Sci. 2002

## Slide 19: AFM of Living Cells: Diatoms I
Gebeshuber I.C. et al. (2003) "Atomic force microscopy study of living diatoms in ambient conditions", J. Microsc. Oxf. 212, pp. 292-299.
AFM
8.8 mm2

## Slide 20: AFM of Living Cells: Diatoms II
Gebeshuber I.C. et al. (2003) "Atomic force microscopy study of living diatoms in ambient conditions", J. Microsc. Oxf. 212, pp. 292-299.

## Slide 21: Underwater Adhesives (AFM)
Most man made adhesives fail to bond in wet conditions, owing to chemical modification of the adhesive or its substrate.
Engineering strong and robust underwater adhesives that are stable in wet environments are a challenge to current technology.
Diatoms produce excellent underwater adhesives.
Diatoms living close to the poles of the earth produce ice binding molecules.

## Slide 22: Underwater Adhesives (AFM)
Gebeshuber I.C. et al. (2002) "In vivo nanoscale atomic force microscopy investigation of diatom adhesion properties", Mat. Sci. Technol. 18, pp. 763-766.
Gebeshuber I.C. et al. (2003) "Atomic force microscopy study of living diatoms in ambient conditions", J. Microsc. Oxf. 212, pp. 292-299.

## Slide 23
To access the adhesive under the diatom  remove cell with STM tip!

## Slide 24: Diatom adhesives

## Slide 25: Biotribology
Technical microsystems often experience failure.
Biological micro- and nanomechanical systems are reliable also at this scale.
© Stanford University
© Mount Allison University, Canada

## Slide 26
© R.W. Crawford, AWI Bremerhaven, Germany

## Slide 27: Biotribology
The aim of biotribology is to gather information about friction, adhesion, lubrication and wear of biological systems and to apply this knowledge to innovate technology, with the additional benefit of environmental soundness.
Gebeshuber I.C. et al. Nanosci. Nanotechnol. 5/1, 79-85 (2005)

## Slide 28: Diatom species interesting for biotribology
Bacillaria paxillifer (old name: B. paradoxa)

## Slide 30
Movie

## Slide 31: Diatom species interesting for biotribology
Ellerbeckia arenaria

## Slide 33: Diatom species interesting for biotribology
Eunotia sudetica

## Slide 35
scale bars
5mm,10mm
50mm, 5mm,10mm
20mm,5mm

## Slide 36
scale bars
50mm,50mm
10mm,5mm
20mm, 5mm

## Slide 37
scale bars
5mm,25mm
50mm,20mm
10mm, 10mm

## Slide 38: AFM of Living Cells: Fibroblasts
© 2000 Radmacher group, Germany

## Slide 39
Single Molecules

## Slide 40: Chaperonins GroEL-GroES
© Cell Press 1996
© http://www.res.titech.ac.jp/~seibutu/ htaguchi/chaperonin/cpn_structure.html
Chaperonins are proteins involved in making certain that other proteins form properly.

## Slide 42: Watching protein-protein interactions in real time
Viani M.B. et al. (2000) Nature Struct. Biol. 7, pp. 644-647
© 2000 Cambridge University Press

## Slide 43: Watching protein-protein interactions in real time
Viani M.B. et al. (2000) Nature Struct. Biol. 7, pp. 644-647

## Slide 44
Atoms

## Slide 45: Nanostructuring atomically flat surfaces with ions

## Slide 46: Omicron UHV AFM/STM

## Slide 47: Atomically flat HOPG crystals before ion bombardement
HOPG, 4*4 nm2 HOPG, 1*1 nm2
STM AFM

## Slide 48: HOPG after ion bombardment
STM, 100.100nm2, HOPG bombarded
with 800 eV Ar+ ions

## Slide 49: Nanodefect aggregation on HOPG steps

## Slide 50: HOPG after ion bombardment
STM, 10.10nm2, HOPG bombarded with 800 eV Ar+ ions
Gebeshuber I.C. et al. (2003) Nucl. Instrum. Meth.
Gebeshuber I.C. et al. (2003) Int. J. Mass. Spectrosc.

## Slide 51: Ion bombardment of atomically flat insulator crystals

## Slide 52: Potential Sputtering
500 eV Ar+ 500 eV Ar7+
UHV AFM contact mode image of sapphire (Al2O3, c-plane 0001) bombarded with ions with the same kinetic, but different potential energy.

## Slide 53: Nanodot formation on Silicon

## Slide 54: Nanodot formation on Silicon

## Slide 55: Ion induced nanodefects on LiF

## Slide 56
Subatomic features

## Slide 57: Atom orbitals (AFM)
The charge distribution in atoms with closed electron shells is spherically symmetric, whereas atoms with partially filled shells can form covalent bonds with pointed lobes of increased charge density.
Covalent bonding in the bulk can also affect surface atoms, leading to four tiny humps spaced by less than 100 picometers in the charge density of adatoms on a (001) tungsten surface.

## Slide 58: Atom orbitals (AFM)
Giessibl and coworkers imaged these charge distributions by means of atomic force microscopy with the use of a light-atom probe (a graphite atom), which directly measured high-order force derivatives of its interaction with a tungsten tip.
This process revealed features with a lateral distance of only 77 picometers.

## Slide 59: Atom orbitals (AFM)
F.J. Giessibl, S. Hembacher, H. Bielefeldt and J. Mannhart (2000) Subatomic features on the Silicon (111)-(7*7) surface observed by atomic force microscopy. Science 289, pp. 422-425.
S. Hembacher, F.J. Giessibl and J. Mannhart (2004) Force Microscopy with Light-Atom Probes. Science 305, pp. 380-383.

## Slide 60: MFRM
Magnetic resonance force microscopy (MRFM) is an imaging technique that acquires magnetic resonance images (MRI) at nanometer scales, and possibly at atomic scales in the future.
MRFM is potentially able to observe protein structures which cannot be seen using X-ray crystallography and protein nuclear magnetic resonance spectroscopy.

## Slide 61: MFRM
Detection of the magnetic spin of a single electron has been demonstrated using this technique.
The sensitivity of a current MRFM microscope is 10 billion times greater than a medical MRI used in hospitals.

## Slide 62: Seeing single spins (AFM)
D. Rugar, R. Budakian, H. J. Mamin and B.W. Chui (2004) Single spin detection by magnetic resonance force microscopy Nature 430, pp. 329-332.

## Slide 63: 3D microscope with atomic resolution
Developed further, the MFRM technique could prove useful for investigating the atomic structure inside materials used in the electronics industry and to image biomolecules - like proteins - at atomic resolution.
However, to reach this goal, nuclear spins have to be detected.
Nuclear spins are harder to detect than electron spins, because a proton´s magnetic moment is 658 times weaker than an electron's.

## Slide 64: ESR-STM
Electron spin resonance-scanning tunneling microscopy (ESR-STM) is a rapidly developing surface-science technique that is sensitive to a single spin existing on or nearby a solid surface.
The single spin is detected through elevated noise at the Larmor frequency that appears when the single spin participates in the tunneling process between the tip and the surface.

## Slide 65: Seeing single spins (STM)
H.C. Manoharan (2002), Spin spotting, Nature 416, pp. 24-25 (Nature News&Views on C. Durkan and M. Welland (2002), Electronic spin detection in molecules using scanning-tunneling-microscopy-assisted electron-spin resonance, Appl. Phys. Lett. 80, 458-460, an article which is reproducing (with different sample) Y. Manassen et al. (1989), Direct observation of the precession f individual paramagnetic spins on oxidezed silicon surfaces. Phys. Rev. Lett. 62(21), 2531-2534)

## Slide 66
Gayatri mantra,
written in Sanskrit
Ellerbeckia arenaria,
the rubberband diatom

## Slide 67
Thank you for your attention !